## Slide 1: Rheometry of Concentrated Suspension of Soft Particles 初探軟顆粒懸浮液流變學：自製流變儀
研究生：
周明叡 Ming-Ruey Chou
指導教授：
蔡日強 博士、黃仲仁 博士 與 陳義裕 博士
Jih-Chiang Tsai, Ph.D. and Jung-Ren Huang, Ph.D. Yih-Yuh Chen, PhD

## Slide 2: Outline
Introduction
Apparatus
Material
Experiment Results
Summary

## Slide 3
L
stationary
rotating
L
L
L
L
Hydrogel spheres / aq. PVC solution
Volume Fraction:  = 0.47-0.64)
L
: Load cells
Side View
23 cm
5.3 cm
13
Bottom View
Introduction

## Slide 4
Chapter2.
Apparatus

## Slide 5
Chapter2.
Apparatus
Force Sensors and Boundaries
Stress Measurement
Driving Motor Control

## Slide 6
+
-
F3
F1
F2
F6
F2
r5=r6
r4
F1
F4
F5
+
-
+
-
+
-
0.225 cm
0.053 m
2.5 Kgw/volt
0.1 Kgw/volt
Force Sensors

## Slide 7
Define: F1＝ F2＝ F3＝ F4＝ F5＝ F6 ≡ 0
Reference points of force measurement:
While top boundary NOT contacting the material yet,
Normal Force:
Torque:
# r4=0.138m, r5=r6=0.211m

## Slide 8
1mm, Distance between boundaries
W(t)
R = 0.1125m
Boundaries
1cm
Acrylic Plates
#Total Volume:

## Slide 9: Charateristic Shear Rate, Shear Strain & Stress
A point P on top boundary rotates with velocity:
Assume Shear Rate is uniform, we have
P
r
h=
Similarly, Shear Strain
Shear Rate
R = 0.1125m

## Slide 10
P
r
Normal Stress :
Shear Stress :
# ,
R = 0.1125m
Also, assume stress is uniform, we have:
Charateristic Shear Rate, Shear Strain & Stress

## Slide 11
Chapter2.
Apparatus
Force Sensors and Boundaries
Stress Measurement
Driving Motor Control

## Slide 12
On Stress Measurement - Noise of a Single Data Point
4 different sample rates, 5000 data points each

## Slide 13
On Stress Measurement - Long Time Stability
Without Load, measure stress over 2+ days

## Slide 14
On Stress Measurement - Reference Point Independence of
Two Components
Impose system with Normal Force Only, see how Torque change
(*Taped water)

## Slide 15
Chapter2.
Apparatus
Force Sensors and Boundaries
Stress Measurement
Driving Motor Control

## Slide 16
Motor Control Overview
Controller
Command
Return
Angular Position
Minimum rotating angle of motor: 0.0001 turn
Precision of the returning = 0.0004 turn,
with sample rate 100-200 Hz

## Slide 17
Motor Motion- Seesaw Mode
Fastest executable angular speed range is limited by the momentum of the upper plate
(with max possible 0.1 turn/s, or from 1.37 s-1)

## Slide 18
Motor Motion- Seesaw Mode
We attempt to achieve sinusoidal motion at early stage…

## Slide 19
Chapter3.
Materials

## Slide 20
Chapter3.
Materials
Materials
Normal Compression Test
-Single Ball
-Suspension
Ball Volume Estimation

## Slide 21
Hydro-gel particles, after swollen mm
Density match with 1.7% PVP solution
(360K Polyvinylpyrrolidone + DI Water)
Materials
dry, d 1mm

## Slide 22
Chapter3.
Materials
Materials
Normal Compression Test
-Single Ball
-Suspension
Ball Volume Estimation

## Slide 23
Measuring head of Anton PaarA Rheometer gives curve
Fit curve with Eq:
Normal Compression Test – Single Ball (S.B)
# Precision of Anton PaarA --- : 0.01N, Z: 0.001mm
: Young’s Modulus; : Diameter of Ball
: Poisson Ratio, = 0.5 ; : 11mm
# Puttock, M., & Thwaite, E. (1969).
Elastic compression of spheres and cylinders at point and line contact

## Slide 24
L
We have:
Stress
Deformation

## Slide 25
Time Dependence of Mechanical Properties of Hydrogel Balls
Using previously described compression test,
We measure 5 balls, once per day, and over 1 month.
*Special thanks to 張睿恩

## Slide 26
Use our rheometer, compress the hydrogel ball suspension, get
Normal Compression Test – The Suspension
Further research, may see:
Lachhab, T., & Weill, C. (1999).
Compression of a soft sphere packing
The European Physical Journal-B
*Special thanks to 費祥霆

## Slide 27
Chapter3.
Materials
Materials
Normal Compression Test
-Single Ball
-Suspension
Ball Volume Estimation

## Slide 28
Estimated Ball Volume
Weight of 50 hydrogel balls:
Density-matched PVP Solution:
Total weight of 50 hydrogel balls
Estimated Single Ball volume
( of Diameter )
From Weight / Density -
In this research, we define
Volume Fraction ϕ
=
#Total Volume:

## Slide 29
α
y(0)
y(t)
2α
L = 4.0m
λ = 6cm
Measure Ball Diameter
by Optical Lever
Assume α small:
*Special thanks to 黃柏嘉

## Slide 30
Measure Ball Diameter
by Optical Lever

## Slide 31
Chapter4.
Experiment Results

## Slide 32
Chapter4.
Experiment Results
Stress Response of the Material
Role of Interstitial Fluid
Plateau and Residual Stress
Time Scales in Relaxation Process
Steady State Measurement

## Slide 33
Stress Response of the Material

## Slide 34
Stress Response of the Material
- Single Cycle
Non-zero
Residual stress
Shear Strain
Shear Rate
Stress

## Slide 35
Residual Stress After Long Waiting Time
Record the residual stress after 25-cycles Seesaw driving

## Slide 36
Chapter4.
Experiment Results
Stress Response of the Material
Role of Interstitial Fluid
Plateau and Residual Stress
Time Scales in Relaxation Process
Steady State Measurement

## Slide 37
Effects of Interstitial Fluid
Residual stress
remains!
WITH NO solution inside:

## Slide 38
Effects of Interstitial Fluid
Residual stress
2 times larger
Start with NO solution, insert 25ml solution each cycle

## Slide 39
Chapter4.
Experiment Results
Stress Response of the Material
Role of Interstitial Fluid
Plateau and Residual Stress
Time Scales in Relaxation Process
Steady State Measurement

## Slide 40
Definition of
Plateau & Residual Stress
Characterize the stress curve by defining two stress value
Plateau (擬穩態應力值, (P)) & Residual Stress(殘餘應力, (R))
Normal Stress-
Symmetric with respect to
Shear in opposite directions
Shear Stress-
Anti-symmetric with respect to
Shear in opposite directions

## Slide 41
Dependence of
Plateau (P) & Residual (R) Stress
On Experiment Parameters
On Maximum
Shear Strain
、

## Slide 42
Dependence of
Plateau (P) & Residual (R) Stress
On Experiment Parameters
On
Shear Rate
、

## Slide 43
Dependence of
Plateau (P) & Residual (R) Stress
On Experiment Parameters
On
Volume Fraction
ϕ
、

## Slide 44
Chapter4.
Experiment Results
Stress Response of the Material
Role of Interstitial Fluid
Plateau and Residual Stress
Time Scales in Relaxation Process
Steady State Measurement

## Slide 45
Time Scales in Relaxation Process

## Slide 46
Time Scales in Relaxation Process
- Single Exponential Fitting
： Time scales of the relaxation Process
: Residual stress at
Fit Normal Stress with
:
Fit Shear Stress with
:

## Slide 47
Time Scales in Relaxation Process
- Single Exponential Fitting

## Slide 48
Time Scales in Relaxation Process
- Double Exponential Fitting
Fit Normal Stress with
Gzz(t):
Fit Shear Stress with
Gxz(t):
： Residual stress at
：Time scales of the relaxation Process

## Slide 49
Time Scales in Relaxation Process
- Double Exponential Fitting

## Slide 50
Double Exponential Fitting
- Sensitive to Initial Parameters
Gzz(t):
Gxz(t):
Compute:

## Slide 51
Double Exponential Fitting
- Sensitive to Initial Parameters
Gzz(t):
Gxz(t):

## Slide 52
Chapter4.
Experiment Results
Stress Response of the Material
Role of Interstitial Fluid
Plateau and Residual Stress
Time Scales in Relaxation Process
Steady State Measurement

## Slide 53
Steady State Measurement
Shear material with a constant rate , with total strain
Average the stress data within , get
1s-1

## Slide 54
Systematic errors in
Steady State Measurement
Same set of parameters but execute with different orders
Re-open the upper boundaries
3
1
2
2
1
3

## Slide 55
Compare the steady state measurement
With Plateau Value

## Slide 56
Summary
Residue stress is created by direct contact, affected mainly by volume fraction and interstitial fluid, not other parameters
Analysis the relaxation process, we can roughly capture at least two relaxation time scale. One of which is around 1s.
Steady state measurement reveals the shear-thinning behavior for ϕ > 0.5, which is close to the ϕ that residual stress is below our apparatus precision.
In steady state measurement, the rate of change of shear rate changes also at time scale 1s.

## Slide 57
Tool used to fix Boundaries

## Slide 58
Effects of Interstitial Fluid

## Slide 59
Phase Average Explanation
1st Period
2nd Period
1st Period
3nd
+
+
dt: Time Window
..…
……
2nd
3rd Period

## Slide 60: Internal imaging at the mid-plane (thru the bottom)
LASER sheet + Nile Blue in particles [Thanks to Joshua Dijksman]
[Ref: Tsai, Voth, and Gollub, PRL 2003]
demo_SS3_20151016_03__vel=100_N=1600_frame820_1199_compressed_combine_Fei1026.avi
50fps @30fps
Movies: ORIGINAL SUBTRACTED

## Slide 61
Yield Strain – Comparing with Oscillatory Shear
 (Pa)
δτ
2max
max