**Laser Writer(DWL66)**



Maskless lithography

Accept .dxf .gds file type

dxf and gds files need to be drawn with " Closure Polyline ".

Sample size: up to 5 inches, minimum size 1cm square (4mm border required)

Minimum line width: 0.7 um

Stable line width: 2 um (using s1813G photoresist)

Alignment error: about 0.5um